ENGINEERING DATA

Table 1

COEFFICIENTS TO BE APPLIED OVER AREAS OF DIFFERENT SURFACES

TO GET EQUIVALENT PLAIN AREA (CPWD)

Sr.No.	Description of Work	Multiplying coefficient

WOOD WORKS – DOORS WINDOWS, 	etc.

1.	Pannelled or framed and braced doors, windows, etc. 	…	1 1/8 (for each side)

2.	Ledged and battened or ledged, battened and braced, doors, windows, etc.	…	1 1/8 (for each side)

3.	Flush door, etc.	…	1 (for each side)

4.	Part paneled part glazed or guazed doors, windows, etc.	…	1 (for each side)

5.	Fully glazed or guazed doors, windows, etc.	…	1/2 (for each side)

6.	Fully venetianed or louvered doors, windows, etc.	…	1 1/2 (for each side)

7.	Trellis (or jaffri) work one way or two way	…	2 (for painting all over)

8.	Carved or enriched work	…	2 (for each side)

9.	Weather boarding	…	1-1/8 (for each side)

10.	Wood shringle rooting	…	1-1/8 (for each side)

11.	Boarding with cover fillets and match boarding	…	1-1/20 (for each side)

12.	Tile and slate battening	…	3/4 (for painting all over)

STEEL WORKS – DOORS, WINDOWS, etc.

13.	Plain sheeted steel doors or windows	…	1 1/8 (for each side)

14.	Fully glazed or guazed steel doors and windows	…	1/2 (for each side)

15.	Part panelled and part glazed or gauzed doors and windows	…	1 (for each side)

16.	Corrugated  sheeted steel doors or windows	…	1 1/4 (for each side)

17.	Collapsible gates	…	1 1/2 (for painting all over)

18.	Rolling shutters of inter coched laths	…	1 1/4 (for each side)

GENERAL WORK

19.	Expanded metal hard drawn steel wire fabric of approved quality, grill

Work and gratings in Gurad Bars, balustrades and paraitions	…	1 (for painting all over)

20.	Open palisade, fencing and gate including standards, braces, rail stays, etc.

In timber or steel	…	1 (for painting all over)

21.	Corrugated iron sheeting in roots, side cladding, etc.	…	1.14 (for each side)

22.	A. C. corrugated sheeting in roofs, side cladding, etc.	…	1.20 (for each side)

23.	A. C. Semi corrugated sheeting in roofs, side cladding, etc.

Or Ninital pattern using plain sheets	…	1.10 (for each side)

24.	Wire guage shutters including painting of wire guage	…	1 (for each side)

2.  HOLLOW CONCRETE BLOCK MASONRY

Table 2

PHYSICAL REQUIREMENTS OF HOLLOW CONCRETE BLOCKS (IS 2185- 1967)

Compressive	Drying shrinkage	Moisture movement	Strength on	Moisture content

strength	     per cent	     per cent	Water absorption	    per cent

kg/cm2			      kg/m2

50	          0.04	         0.03	        240		         40

Table 3

Minimum thickness, mm, of load-bearing walls for hollow concrete block masonry (IS 2572- 1963)

Wall location	One-storeyed building	Two-storeyed building	Three-storeyed building

Third Storey	-	-	200

Second storey	-	200	200

First storey	200	200	300

Basement	200	300	300

Table 4

PROPORTION OF COARSE AGGREGATE FOR CONCRETE

i)	40 mm and down size	ii)	20 mm and down size	iii)	12mm and down size

40 mm	50% ± 5%		20 mm	66% ± 6%		12mm	60% ± 5%

20 mm	25% ± 3%		10 to 12mm	34% ± 4%		10 mm	25% ± 3%

10 to 12mm	25% ± 2%					4.75 mm	15% ± 2%

Table 5

WORKABILITY OF CONCRETE:

The concrete mix proportions chosen should be such that the concrete is of adequate workability for the placing conditions of the concrete and can properly be compacted with the means available.  Suggested ranges of workability

Of concrete measured in accordance with IS 1199 are given below:

Placing Conditions	 Degree of workability	Slump (mm)

(1)		(2)		(3)

Blinding concrete;	 Very low	See Note

Shallow sections;

Pavements using pavers

Mass Concrete;	    Low	  25-75

Lightly reinforced sections in slabs,

beams, walls, columns;

Floor’s

Hand placed pavements;

Canal lining;

Strip footings

Heavily reinforced sections in slabs,	   Medium	50-100

beams, walls columns;		75-100

Slipform work;

Pumped concrete

Trench fill;	    High	100-150

In-situ piling

Tremie concrete	  Very high	See Note

NOTE	(i)	:	For most of the placing conditions, internal vibrators (needle vibrators) are suitable. The diameter of the needle shall be determined based on the density and spacing of reinforcement bars and thickness of sections. For tremie concrete, vibrators are not required to be used.

(ii)	:	In the ‘very low’ category of workability where strict control is necessary, for example pavement quality concrete, measurement of workability by determination of compacting factor will be more appropriate than slump and a value of compacting factor of 0.75 to 0.80 is suggested.

Table 6

6.1.	STRIPPING TIME:

For Portland cement	For Pozzolana cement

a)	Walls, columns & vertical surfaces of all structural members	16-24 hours	72 hours

b)	Slabs (props. Left under)	3 days	35 days

c)	Beams (props. Left under)	7 days	45 days

d)	Removal of props under slab

- Spanning upto 4.50 mtr.	7 days

- Spanning over 4.50 mtr.	14 days

e)	Removal of props under beams and arches

- Spanning upto 6.0 mtr.	14 days

- Spanning over 6.0 mtr.	21 days

6.2.	METHOD OF DE-CENTERING:

1)	For continuous or simply supported structures the decentering shall be affected from the centre of the span

(minimum shear force zone) towards the supports.

2)	For cantilever structures, the de-centering shall be affected from the free end (minimum shear force zone) towards the supports.

6.3.	VERTICAL ALIGNMENT OF COLUMN:

The eccentricity should not be more than 5% of the column face width.

Table 7

PHYSICAL REQUIREMENTS OF CEMENT

Type of Cement	Ordinary	Rapid-	Low heat	Portland	Portand	High	Super-

Portland	hardening	Portland	blast-furnace	pozzolana	alumina	sulphated

slag

Indian Standard	269-1967	269-1967	269-1967	455-1967	1489-1967	6452-1972	6909-1973

Fineness	Residue by weight	>10%	>5%	---	>10%	>5%	---	---

On 90-micron is

Sieve

Minimum specific

Surface (Blaine’s

Air permeability),

Cm2/gm	2.250	3.250	3.200	2.250	3.000	2.250	4.000

Soundness	Expansion1 (Le	>10mm	>10mm	>10mm	>10mm	>10mm	>5mm	>5mm

Chatelier)

Autoclave test2	0.8%	>0.8%	>0.8%	>0.8%	>0.8%	---	---

Setting	Initial	<30min	<30min	<60min	<30min	<30min	<30min	<30min

Time	Final	>600 min	>600 min	>600 min	>600 min	>600 min	>600 min	>600 min

Maximum	24 hours	---	160	---	---	---	300	---

Compres-

Sive	72 hours	160	275	100	160	---	350	150

Strength	168 hours	220	---	160	220	220	---	220

(Kg/cm2)	672 hours	---	---	350	---	310	---	300

Minimum	24 hours	---	---	---	---	---	---	---

Tensile	72 hours	---	---	---	---	---	---	---

Strength				Heat of		Average drying

(Kg/m2)				hydration to be	shrinkage of

not more than	mortars to be not

65 cal/gm at 	more than 0.15

7 days and 75	per cent

cal/gm at 28 day

| Table 8 REDUCTION IN STRENGTH OF CONCRETE MADE WITH STORED CEMENT | Table 9 RATE OF HARDENING OF CONCRETE MADE WITH FRESH AND STORED CEMENT |
| --- | --- |
| Period of storage of Minimum expected reductions in Cement strength at 28 days, per cent | Testage 1:5 concrete made with 1:5 concrete made Cement stored in bags with fresh cement, Under normal conditions per cent for 6 months, per cent |
| Fresh 0 3 months 20 6 months 30 1 Year 40 2 years 50 |  |
|  | 7 days 73 100 28 days 75 100 6 months 84 100 |
| Note : If cement is likely to have deteriorated during storage, it should be sent to laboratory for Test |  |

Table 10

RECOMMENDED MIXES FOR VARIOUS TYPES OF CONSTRUCTION

Type of work	Recommended	Maximum	water in litres

Mix (by volume)	size of agg-	per bag of

regate mm	cement

Long span arches, heavily loaded columns	1:1:2	12 to 20	16 to 18

Heavily stressed members; small precast works, such as	1:2:2	12 to 20	20 to 23

posts and poles for fencing, telegraphs, signals, garden

furniture and decorative and other items of work of very thin

sections; watertight construction for high heads; long piles

Columns and members subjected to medium load walls and	1:2:3

floors of reservoirs and tanks; cisterns, sewers, well keros,	  or	    20	     25

platforms and other watertight constructions for moderate	1:1½:3

heads; non-surfaced roof slabs; concrete deposited under

water

General building work subjected to ordinary stresses such as	1:2:4	12 to 40	27 to 30

beams, slabs, columns, panel walls, basement and retaining		as required

walls, stairs, lintels and sills; pavements, driveways, and

side walks; floors; steps; bunkers and silos; bridges, dams,

piers, etc., exposed to action of water and frost; machine

foundations subject to vibrations; footings, piles

Mass concrete work in culverts, retaining walls, compound	1:3:6	25 to 50	     34

walls and ordinary machine bases; foundation walls which

need not be watertight

Mass concrete for heavy walls; foundations under column	1:4:8	40 to 75	45 to 48

footings and under heavy duty floors

Table 11

BULKING OF SANDS FOR VARIOUS MOISTURE CONTENTS

Moisture, per cent	Percentage bulking in

fine sand	medium sand	coarse sand

1	16	 8	 6

2	26	16	12

3	32	22	15

4	36	27	17

5	38	29	18

6	37	28	18

8	35	26	16

10	32	22	12

12	28	19	 8

15	22	12	 2

17	18	 7	 0

20	 9	 0	 0

27	 0	 0	 0

Table 12

MANPOWER AND MATERIALS REQUIREMENTS IN RESIDENTIAL BUILDINGS

Table A – Equation for Materials Requirement (A is the plinth Area in m2)

Equations

Material	Single Storey		Double Storey	Four Storey

(R.C.C. Framed)

Bricks (% Nos.)	2.26A+66.8	2.15A+63	-26.2+2.56A-0.0096A2

Cement (Tonne)	0.153A+0.57	0.145A+0.54	0.182A-0.35

Steel (Kg)	21.3A-314	21.97A-305	-1491+92.0A-0.36A2

Sand (m3)	0.47A-7	0.376A-5.6	0.361A-0.38

Coarse aggregate

(i)  20 mm and down (m3)	0.176A-0.21	0.178A-0.21	0.295A-0.75

(ii)  40 mm and down (m3)	0.145A+1.5	0.075A+0.78	0.45+0.002A+0.0001A2

Brick Aggregate (m3)	0.113A+0.83	0.056A-0.42	0.021A+0.01

Timber Frames and Shutters (m3)	0.019A+0.23	0.019A+0.23	0.02A+0.11

Timber shuttering (m3)	0.0042A	0.0042A	0.009A-0.03

Ballies (m)	0.504A	0.504A	0.90A-2.41

Lime (quintal)	0.145A-0.35	0.073A-0.17	0.063A-0.08

Surkhi (m3)	0.052A-0.37	0.026A-0.18	0.01A

Bitumen (kg)	1.836A-9	0.918A-4	0.357A+14

Glass (m2)	0.064A-0.73	0.064A-0.73	0.056A-0.06

Primer (Lt)	0.068A	0.068A	0.061A+0.56

Paint (Lt)	0.108A+0.27	0.108A+0.27	0.085A+1.93

* Equations for super-structure only. For sub-structure refer Table C

Table B – Equation for Labour Requirement (A is the plinth Area in m2)

Labour	Equations

Single Storey		Double Storey	Four Storey

(R.C.C. Framed)

Mason (days)	1.335A+28	1.335A+26	1.97A-2

Carpenter (days)	1.184A-9	1.194A-9	1.61A

Painter (days)	0.089A	0.089A	0.09A

Blacksmith (days)	0.0269A-4	0.0274A-4	-16+1.01A-0.004A2

Mazdoor (days)	4.769A+32	4.91A+33	5.49A-9.2

* Equations for super-structure only. For sub-structure refer Table C

| Table c – Equations for Materials and Labour Requirements for Substructure in Four Storeyed (R.C.C Framed) Building | Table D – Equations for Materials and Labour Requirements for Additonal one Metre depth of Foundaton |
| --- | --- |
| Materials / Labour Equations Materials Cement (tonne) 0.0204A-0.014 Sand (m3) 0.036A Coarse Aggregate 20 mm and down (m3) 0.071A-0.01 Steel (kg) -171+10.46A-0.041A2 Timbers-shuttering (m3) 0.0007A Ballies (m) 0.036A+0.06 Labour Mason (days) 0.023A Carpenter (days) 0.05A Blacksmith (days) -1.6+0.1A-0.0003A2 Mazdoor (days) 0.343A | Materials / Labour Equations Materials Cement (tonne) 0.0022A+0.002 Sand (m3) 0.0031A+0.015 Coarse Aggregate 20mm and down (m3) 0.0053A+0.02 Steel (kg) -17.9+1.118A-0.004A2 Timbers-shuttering (m3) 0.0002A Ballies (m) 0.018A+0.95 Labour Mason (days) 0.006A Carpenter (days) 0.024A Blacksmith (days) 0.006A Mazdoor (days) 0.086A |

Materials required on plinth area basis of single storey building

i)	Brick	-	250 to 300 Nos. per sq. mtr. of Plinth Area

ii)	Cement	-	3.5 to 4.0 Bags per sq.mtr. of Plinth Area

iii)	Steel	-	12 to 15 kgs. Per sq. mtr. of Plinth Area

Table E – Percentage cost of various components of Building work

% of the	% of the

Whole cost	Whole cost

Cost of Labour Materials:		Cost of sanitary and electrical works	8

i)	Cost on account of labour	30 to 35		 i)	Sanitary and water supply works	4

ii)	Cost on account of materials	70 to 65		ii)	Electrical installation excluding Fan	4

Direct over Head Cost		Cost of materials and labour required for building,

Percentage distribution

i)	Direct cost on a actual work (job)	85

ii)	Overhead cost due to establish-				  i)	Cost of brick	22

ment, supervision, incidentals, etc	15		 ii)	Cost of Cement	12

iii)	Cost of foundation and plinth	10 to 15		iii)	Cost of steel bars	10

iv)	Cost of super structure	90 to 85		iv)	Cost of timber	10

Cost of Second Storey	85 to 90		 v)	Cost of Other materials	14

vi)	Wages of labour	30

Cost of different parts or percentage break up of		vii)	Work charged establishment	  2

Building (excluding sanitary and electrical works)				Total   100

i)	Earth work in excavation and filling	  ½

ii)	Concreting in foundation	  5

iii)	Damp proof course	  1

iv)	Brick work	 34

v)	Roofing	 20

vi)	Flooring	  6

vii)	Doors and Windows	 16

viii)	Plastering and Pointing	 10

ix)	White washing, colour washing,

painting, etc.	   2

x)	Miscellaneous	  5½

Total	100

Note :	If the estimated cost of the building and rates of materials are known the approximate quantities of materials		can be calculated.  Cost can be calculated approximately on plinth areas basis also.

Table 13

MATERIAL REQUIREMENTS FOR FINISHED ITEMS OF WORK

Granite metal	Mortar		Cement or

Sl.	Description of work	Unit	stones, bricks	or sand			Lime

No.			  tile etc.(in cum)	(in cum)	Bags	 Kgs.

1			2			 3		4	5		6		    7

1.	CONCRETE

a)  Lime Concrete 1:2:4	One Cum	0.90	 0.45	    0.225

b)  Cement Concrete 1:1:2		“	0.76	 0.38	10.815 (9.96)	541 (498)

c)  Cement Concrete 1:1½:3		“	0.85	0.416	 8.30 (7.86)	415 (393)

d)  Cement Concrete 1:2:4		“	0.90	 0.45	6.475 (6.02)	324 (301)

e)  Cement Concrete 1:3:6		“	0.90	 0.45	 4.55 (4.16)	228 (208)

f)  Cement Concrete 1:4:8		“	0.96	 0.48	 3.50 (3.16)	175 (158)

g)  Cement Concrete 1:5:10		“	1.00	0.491	2.975 (2.52)	149 (126)

h)  Cement Concrete 1:7:12		“	1.00	 0.50	2.300 (2.04)	115 (102)

Note :  The values within the brackets are for unfinished items of work.

2.	R. C. C. Plan Chejja of 7.5 cm

ac. Thickness using 1:2:4, etc.	 10 Sqm.	 0.75	 0.375	4.90	   	   245

3.	-do- Box Type Chejja –do-	 10 Sqm.	0.375	 0.562	6.00	      300

4.	Reinforced drop chejja or reinforced

facia 5 cm. thick by providing and fixing

chicken mesh and plastering with

C. M. 1:3 including steel (steel required

6mm dia 16 kgs.per 10 Sqm.)	 10 Sqm.	  ---	  0.50	5.00	      250

5.	Reinforced backing to cupboards for

partition walls with reinforcements and

chicken mesh and plastering with C.M.

1:3 finished thickness 5 to 6 cm. (steel

required 6mm dia 16 kgs. Per 10 Sqm.)	  10 Sqm.	  ---	  0.50	5.00	250

6.	R.C.C. racks with C.C. 1:2:4 proportion

5cm, thick with reinforcement, etc, as

per specification (steel required 26kgs /

10 Sqm. (6mm dia)	  10 Sqm.	 0.45	 0.225	3.24	162

7.	R.C.C. Loft (Atta) 7.5 cm, thick with C.C.

1:2:4 concrete, etc.	  10 Sqm.	 0.75	 0.375	6.25	312

8.	R.C.C. perforated ventilators 4 cm thick

inclusive of steel (steel required

6 mm dia 32.9 kgs. per 10 Sqm.)	  10 Sqm.	  ---	 0.350	5.00	250

9.	R.C.C. fins with C. M. 1:3 Plastering

(including steel)	  10 Sqm.

a) 5 cm thick [Steel reqd. 44.60 kgs. per

10 Sqm. Ie., 38 kgs.

(10mm) and 6.6 kgs. (6 mm)]	  10 Sqm.	  ---	  0.50	5.00	250

b) 7.5 cm thick (steel reqd. –do-)	  10 Sqm.	  ---	  0.75	7.50	375

10.	R.C.C. Slabs with C.C. 1:2:4, 5 cm, thick,

etc. for wall shelves	  10 Sqm.	  0.50	  0.25	3.50	175

11.	Precast or cast-in-situ work in

C.M. 1:3, etc.

a) 5 cm thick	  10 Sqm.	  ---	  0.50	5.00	250

b) 7.5 cm thick	  10 Sqm.	  1.00	  0.50	8.00	400

12.	R.C.C. 1:2:4 Parapet solid or perforated

a) 7.5 cms thick	  10 Sqm.	 0.075	 0.375	6.25	312

b) 10 cms thick	  10 Sqm.	   0.10	   0.50	8.00	400

1			2			         3		      4	     5	       6		    7

13.	R.C.C. 1:2:4 work with 6 mm M.S. Rods

a) 10 cm thick (Steel Qty. 20 kgs/ 10 Sqm.)  10 Sqm.	  1.00	  0.50	 8.00	400

b) 12.5cm thick (Steel Qty. 20 kgs/10Sqm.)  10 Sqm.	  1.25	  0.50	10.40	520

c) 15 cm thick (Steel Qty. 20 kgs/10 Sqm.)	   10 Sqm.	  1.50	  0.73	12.50	625

14.	Stone Masonry:

i) Rubble Stone masonry (uncoarsed) for

foundation.

a) – do – in C.M. 1:8	 One cum	  1.05	  0.34	1.258	 63

b) – do – in C.M. 1:6	       “	  1.05	  0.34	1.666	 83

c) – do – in C.M. 1:4	       “	  1.05	  0.34	2.516	126

d) – do – in gauged mortar 1:1:9	       “	  1.05	  0.34	0.97	 49

e) – do – in gauged mortar 1:1:8	       “	  1.05	  0.34	1.11	 56

f) – do – in gauged mortar 1:1:6	       “	  1.05	  0.34	0.44	 72

ii) Granite size stone masonry with

stones hammer dressed for foundation

a) – do – in C.M. 1:8	 One cum	  1.05	  0.28	1.44	 85

b) – do – in C.M. 1:6	       “	  1.05	  0.28	1.424	 71

c) – do – in C.M. 1:4	       “	  1.05	  0.28	2.12	106

d) – do – in gauged mortar 1:1:9	       “	  1.05	  0.28	0.79	 40

e) – do – in gauged mortar 1:1:8	       “	  1.05	  0.28	0.94	 47

f) – do – in gauged mortar 1:1:6	       “	  1.05	  0.28	1.18	 59

15.	 i) Granite size stone masonry, edges of

stones chistle dressed for basement/

superstructure/Arch work

a) – do – in C.M. 1:8	 One cum	  1.10	  0.28	1.04	 52

b) – do – in C.M. 1:6	       “	  1.10	  0.28	1.424	 71

c) – do – in C.M. 1:4	       “	  1.10	  0.28	2.120	106

ii) Ashlar masonry for superstructure

a) – do – in C.M. 1:4	 One cum	  1.10	  0.28	1.94	 47

b) – do – in C.M. 1:3	       “	  1.10	  0.28	1.20	 60

16.	Brick masonry with modular bricks for

basement and superstructure

a) – do – in C.M. 1:8	 One cum	500 Nos.	  0.27	1.021	 51

b) – do – in C.M. 1:6	       “	500 Nos.	  0.27	1.363	 68

17.	Brick masonry with table moulded bricks

for basement and superstructure

i) a) – do – in C.M. 1:8	 One cum	500 Nos.	  0.22	0.935	 47

b) – do – in C.M. 1:6	       “	500 Nos.	  0.22	1.24	 62

c) – do – in C.M. 1:4	       “	500 Nos.	  0.22	1.87	 94

d) – do – in C.M. 1:3	       “	500 Nos.	  0.22	2.44	122

ii) a) in gauged mortor in 1:1:9	 One cum	500 Nos.	  0.20	0.79	 40

b)       - do -	 1:1:8	       “	500 Nos.	  0.20	0.935	 47

c)       - do - 	 1:1:6	       “	500 Nos.	  0.20	1.18	 59

18.	Wire cut modular brick for basement and

super structure.

a) – do – in C.M. 1:8	 One cum	500 Nos.	  0.20	0.74	 37

b) – do – in C.M. 1:6	       “	500 Nos.	  0.20	1.01	 51

c) – do – in C.M. 1:4	       “	500 Nos.	  0.20	1.515	 76

19.	Arch work with approved quality of table

moulded bricks in C.M. 1:4	 One cum	500 Nos.	  0.20	1.48	 74

20.	a) Partition walls with modular bricks in

C.M. 1:4 10 cm thick with M.S, reinforcements

(steel reqd. 6mm dia. 18 kgs per 10 Sqm.)	    10 Sqm.	500 Nos.	  0.27	2.00	100

b) –do- with table moulded bricks in C.M. 1:4,

10 cms thick with M.S. reinforcements.

(Steel reqd. 6mm dia 18 kgs. per 10 Sqm.)	    10 Sqm.	500 Nos.	  0.27	2.00	100

REQUIREMENT OF MATERIALS, LABOUR FOR PAINTING WORKS

[FOR AN AREA OF 10 SQM]

A. Primary coat on new wood works

White lead	….	0.60 kg	Painter I class	….	0.70 No.

Whiting	….	1.00 kg	Brush, soap, etc.	….	L.S.

Linseed oil (twice boiled)	….	0.61 lit

B. Primary coat on new iron work

Red Lead	….	1.00kg	Painter I class	….	0.70 No.

Patent drier	….	15.30 mg	Brush, soap, Putty, etc.	….	L.S.

Boiled Linseed oil	….	0.46 lit

C. Primary coat on new plastered surface

Red Lead	….	0.55 kg	Painter I class	….	0.70 No.

White Lead	….	0.55 lit	Brush, soap, Putty, etc.	….	L.S.

Boiled Linseed oil	….	0.60 lit

D. Best Varnishing wood work		One Coat		Two Coats

Best Varnish		0.77 lit		1.20 lit

Linseed oil (boiled)		0.60 lit		0.90 lit

Painter I class		0.70 No.		1.10 No.

Mazdoor I class		0.70 No.		1.10 No.

Brush, Soap, etc.		L.S.		L.S,

E. Bees Wax

Bees wax	….	0.12 kg	Painter I class	….	1.10 No.

Turpentine	….	0.18 lit	Sundries		….	L.S.

F. Painting new wood work, two coats over a priming

Primer	….	1.44 lit	Painter I class	….	1.90 No.

Paint	….	2.55 lit

G. Painting New iron work

Red oxide	….	0.33 lit	Painter I class	….	1.80 No.

Enamel Paint	….	2.20 lit

H. Painting old wood work

One coat paint	….	1.33 lit	Painter I class	….	0.70 No.

Two coats paint	….	2.22 lit	Painter I class	….	1.20 No.

I. Painting old iron works

One coat paint	….	1.11 lit	Painter I class	….	1.70 No.

Two coats paint	….	1.89 lit	Painter I class	….	2.10 No.

J. Cement Paint two coats

Cement paint	….	3.23 kgs.	Painter I class	….	0.50 No.

Mazdoor I class	….	0.50 No.

Mazdoor II class	….	0.80 No.

K. Plastic emulsion Paint-two coats over priming coat

Primer	….	0.98 lit	Painter I class	….	2.20 No.

Plastic emulsion	….	1.40 lit

1		2	3	4	5	6	7

21.	FLOORING

i).	With C.C. 1:2:4, 40mm thick and top

plastered with C.M. 1:3, 12mm thick	10 Sqm.	  0.36	0.31	3.90	195

ii)	With C.C. 1:2:4, 40mm thick on a bed

of 15 cm thick 1:5:10 C.C, bed with

C.M. 1:3, 12mm thick top plastering	10 Sqm	  1.86	1.06	8.36	418

iii)	With C.C. 1:2:4, 40mm thick on a bed

of 10cm thick 1:4:8 C.C. bed with C.M.

1:3, 12mm thick top plastering	10 Sqm.	  1.32	0.79	7.40	370

iv)	Wich C.C. 1:2:4, 40mm thick on a bed

of 1:4:8 C.C. 15cm thick and top

plastered with C.M. 1:3, 12 mm thick	10 Sqm.	  1.80	1.03	9.15	458

v)	With Mosaic tiles grey colour fixed in

C.M., 1:3, 20mm thick over a bed of 10 cm

thick C.C. 1:4:8 and pointed with white cement

(Mosaid tiles 250 x 250mm size 155 Nos.)	10 Sqm.	  0.96	0.68	5.50	275

vi)	- do – without cement bed (155 Nos.)	10 Sqm.	   ---	0.20	2.00	100

vii)	With white adanga Marble tiles fixed in C.M.

1:3, 20mm thick on existing concrete

bed and pointed with white cement	10 Sqm.	   ---	0.20	2.00	100

viii)	Dadooing with galzed tiles of size

150 x 150mm set in C.M. 1:3 and pointed

with white cement	10 Sqm.	  450 Nos.	0.20	2.00	100

ix)	 - do – 100 x 100 mm size tiles. – do - 	10 Sqm.	 1000 Nos.	0.20	2.00	100

22.	PLASTERING

i)	Plastering to Stone masonry in C.M. 1:6

20 mm thick	10 Sqm.	   ---	0.22	1.09	 55

ii)	Plastering to Stone masonry in C.M. 1:4

20mm thick	10 Sqm	   ---	0.22	1.66	 83

iii)	Plastering to Burnt brick masonry (Plain

Plastering) in C.M. 1:6

a) 20mm thick	10 Sqm.	   ---	 0.2	1.00	 50

b) 12mm thick	10 Sqm	   ---	0.12	0.70	 35

iv)	Plastering to B.B. masonry (Plain

Plastering) in C.M. 1:6

a) 20mm thick	10 Sqm.	   ---	0.20	1.52	 76

b) 12mm thick	10 Sqm.	   ---	0.13	0.99	 50

v)	Plain Plastering to concrete in C.M. 1:6

a) 20 mm thick	10 Sqm.	   ---	0.20	1.00	 50

b) 12 mm thick	10 Sqm.	   ---	0.13	0.70	 35

vi)	Plain Plastering to concrete in C.M. 1:4

a) 20mm thick	10 Sqm.	   ---	0.20	1.52	 76

b) 12mm thick	10 Sqm.	   ---	0.13	0.97	 49

vii)	Plain Plastering to concrete in C.M. 1:3

a) 20mm thick	10 Sqm.	   ---	0.20	2.00	100

b) 12mm thick	10 Sqm.	   ---	0.13	1.31	 66

viii)	Pointing in C.M. 1:3

a) 20mm thick	10 Sqm.	   ---	0.02	0.20	 10

23.	CEMENT MORTARS

Cement					Cement

a)	Cement and Sand Mortar	  Kgs.	Bags	b) Gauged Mortar	Kgs.	Bags

1.1	1cmtr	1033.0	20.66	    (Cement lime and Sand Mortar

1.2		  682.0	13.64	1:1:6	1 cmtr	239.0	4.78

1.3	  481.0	  9.82	1:1:8	185.0	3.70

1.4	  373.0	  7.46	1:2:9	160.0	3.20	1.6	  248.0	  4.96	1:5:10	144.0	2.88

1.8	  188.0	  3.76	1:7:12	118.0	2.36